- General specifications for terminals.

- Terminals must be made of brass by the method of casting or die stamping. Terminals which are made of brass tape must meet the following characteristics: tubular terminals are made of hard or half-hard brass, all the rest – made of soft brass.

- Terminals must not have: burs more than 0, 1 mm long, splits, signs of corrosion and other drawbacks.

- Sharp corners and edges may be rounded off with radius less than 0, 5 mm.

- Hole fork symmetry relatively line of symmetry may be not more than 0, 25 mm.

- Bend angles deviation of terminals made of brass tape must be less than 5 degrees, difference of clutches height must be less than 0, 5 mm.

- While being  armored the terminals must not split, allowing swaging diametrically.

- If a terminal has a polarity sign, it should be made by method of indentation up to 1 mm in depth. The sign should be distinctly seen.

- Terminals covering by method of tinplating or chemical passaging.

- Terminals made of brass tape must be delivered as a chain with tapes, all the rest – apiece.